## Slide 1
Characterization of Long Bent Silicon Crystals for Channelling Applications at the LHC
Thesis Project
ANNA SOFIA MORO
Update 24 August 2026

## Slide 2: WHAT IS ‘CHANNELING’ IN CRYSTALS?
Channeling effect
Charged particles get trapped and guided between regular atomic planes
Beam deflection
Bending the crystal physically steers the beam’s trajectory
Advantage
A compact alternative to traditional magnets for deflecting or extracting beams
THE PHYSICS
Entry condition: the Lindhard angle
a particles enters the channel only if its incidence angle is within of the crystal plane
Notes: Inside a crystal, atoms are arranged in regular planes. If a charged particle enters nearly parallel to these planes, it can become trapped and guided along their curvature, “locked” to the lattice instead of crossing it in a straight line.
When the crystal is bent, the channeled beam is deflected along with the grating: the crystal acts as a guide, offering a compact alternative to traditional magnets for deflecting or extracting a particle beam.

## Slide 3: THE TWOCRYST EXPERIMENT
THE PROJECT

## Slide 4: MY ANALYSIS
THE PROJECT
DATA
2024 dataset for two long crystals
180 GeV beam (70% protons and 30% pions)
GOAL OF MY WORK
Measure the channeling efficiency and the crystal torsion on newly fabricated long crystals.
WHAT IS NEW
ggg
My work takes place on the SPS – H8 test bench, where individual crystals are characterized before being used.

## Slide 5: MY ANALYSIS
EXPERIMENTAL SETUP
DATA
2024 dataset for two long crystals
180 GeV beam (70% protons and 30% pions)
My work takes place on the SPS – H8 test bench, where individual crystals are characterized before being used.
silicon microstrip sensors
long crystal

## Slide 6: THE ANALYSIS PIPELINE
METHOD
Analysis implemented in Python on RDataFrame (ROOT).
QUALITY FILTERS
Selecting single tracks, alignment check between the upstream and downstream telescope arms
CRYSTAL EDGES
Reconstruct the (x,y) spatial window illuminated by the crystal
(2 independent methods)
TORSION MAP
2D checkerboard grid analysis of the entrance face:
surface fit to obtain
LINDHARD CUT
Selecting particles entering within , corrected point-by-point for torsion
EFFICIENCY
and the full error budget (statistical and systematic errors)

## Slide 7: ANALYSIS: DETECTOR ALIGNMENT
PRELIMINARY ANALYSIS
QUALITY FILTERS
Selecting single tracks, alignment check between the upstream and downstream telescope arms
To ensure that the upstream and downstream detectors are aligned, we check the deviation between the initial and final positions of particles that definitely did not hit the crystal, ensuring that is zero.
We can also check the alignment by doing a linear fit between the upstream and dowstream profiles.

## Slide 8: ANALYSIS: CRYSTAL EDGES
PRELIMINARY ANALYSIS
CRYSTAL EDGES
Reconstruct the (x,y) spatial window illuminated by the crystal
(2 independent methods)
METHOD 1: CHANNELED PARTICLES
Isolate already channeled particles (only uses ~ 20% of data)
Their impact position (x, y) traces the crystal footprint, matching its expected dimension
METHOD 2: MULTIPLE COULOMB SCATTERING
Notes: Results: the two methods agree on a width of 2 mm in x, in y the scattering method shows a narrower effective window due to the clamps, consistent with the torsion analysis, which already excludes the poorly-illuminated edges

## Slide 9: ANALYSIS: CRYSTAL EDGES
PRELIMINARY ANALYSIS
CRYSTAL EDGES
Reconstruct the (x,y) spatial window illuminated by the crystal
(2 independent methods)
METHOD 1: CHANNELED PARTICLES
METHOD 2: MULTIPLE COULOMB SCATTERING
Particles that physically crosses the crystal picks up extra Coulomb scattering, the ones outside the crystal do not
The width of the outgoing angular distribution is measured
A sharp transition marks the edges
Notes: Results: the two methods agree on a width of 2 mm in x, in y the scattering method shows a narrower effective window due to the clamps, consistent with the torsion analysis, which already excludes the poorly-illuminated edges

## Slide 10: ANALYSIS: MAPPING THE TORSION
PRELIMINARY ANALYSIS
TORSION MAP
2D checkerboard grid analysis of the entrance face:
surface fit to obtain
The torsion effect is not negligible in long crystals and must be accounted for
The crystal is not perfectly rigid: the orientation of the crystalline planes rotates slightly across its surface
The optimal entry angle is therefore not unique, but varies point by point
Beam spot divided into a 0.1 mm (x,y) grid
RESULTS:
ggg
Angular scan
for each cell
local
that maximize
efficiency
Surface fit
(parabolic)
to extract the
global

## Slide 11: CHANNELING EFFICIENCY
ANALYSIS
CHANNELING EFFICIENCY
Notes: By fitting only the right side of the peak, we ensured the cleanest possible measurement by excluding any contribution from dechanneled particles.

## Slide 12: CHANNELING EFFICIENCY: RESULTS
ANALYSIS
RUN 8430 (REFERENCE)
long crystal 1 |  | 
long crystal 2 |  | 
long crystal 1 |  | 
long crystal 2 |  | 
Chart: Channeling efficiency [%]
| run 8430 | run 8431 | run 8650 | run 8655 | run 8656
High | 19.8 | 19.4 | 17.3 | 18.2 | 18.2
Low | 19.4 | 19 | 16.9 | 17.8 | 17.8
Close | 19.6 | 19.2 | 17.1 | 18 | 18
crystal 1 crystal 2
anomalous run

## Slide 13: CHANNELING EFFICIENCY: RESULTS
ANALYSIS
Long crystal 1
Long crystal 2
ERROR BUDGET
Statistical error:
Binomial error
Fit errors
Systematic error:
Fit model choice
Binning choices

## Slide 14: CHANNELING EFFICIENCY: RESULTS
ANALYSIS
long crystal 1 |  | 
long crystal 2 |  | 
long crystal 1 |  | 
long crystal 2 |  | 
On article …
It was found and efficiency of and a torsion of for the TCCP long crystal.

## Slide 15: WHAT’S NEXT: SIMULATION
NEXT STEPS

## Slide 16: 2. PREVIOUS ANALYSIS: CRYSTAL EDGES
To define the true footprint at the entrance face we must project the downstream edges back upstream.
We need to subtract a shift from the downstream edge position.
Channeled particles follow the bent lattice planes, resulting in a lateral geometric drift along the -axis as they traverse the crystal.
Notes: While the crystal edges are identified using the downstream particle profiles (where channeled particles are distinctly separated), our subsequent analysis strictly requires upstream coordinates.
Channeled particles follow the bent lattice planes, resulting in a lateral geometric drift along the x-axis as they traverse the crystal. To define the true physical footprint at the entrance face, we must project the downstream edges back upstream.

## Slide 17: 3. ANALYSIS: TORSION EFFECT
Torsion effect: in long crystals (>1 cm), structural torsion is non-negligible and must be incorporated into the analysis.
The different orientations of the crystallographic planes along the crystal front surface influence the angular range in which particles can be channelled.
Before selecting the particles that have entered with the right angle (within ) we need to apply a correction because the cut may not be centered at zero.
We do not choose a single value but rather in order to also apply a torsion correction which is not negligible in the long crystals.
Notes: torsion is the variation of the crystalline plane orientation along the y direction perpendicular to the bending plane
: the angle where the crystal planes are perfectly aligned with the beam.
𝜃_0: the angle where the crystal planes are perfectly aligned with the beam.

## Slide 18: 4. FINAL RESULTS
Crystal 1 does show inconsistencies in different runs (8430 and 8650 have different energies)
Crystal 1 shows a maximum efficiency of
Crystal 2 shows a maximum efficiency of
Notes: CONSISTENT ACROSS DIFFERENT RUNS FOR THE SAME CRYSTALS

## Slide 19: BACKUP SLIDES

## Slide 20: SCHEMATIC LAYOUT
Station 1
z ~ -12.4 m
Station 2
z ~ -10.4 m
crystal
z = 0 m
Station 3
z ~ 0.5 m
Station 4
z ~ 4.7 m
Incoming arm vacuum pipe
Downstream arm vacuum pipe
Beam
direction
Beam: H8 secondary beamline off the SPS, driven by 400 GeV protons
Spectrometer selection 180 GeV hadrons (30% and 70% )
Trackers:
2 silicon microstrip sensors
639 strips, 98 mm length
with a ~ 7 um resolution
BACKUP SLIDE

## Slide 21: SCHEMATIC LAYOUT
BACKUP SLIDE

## Slide 22: SPATIAL CUT
2 mm
12.8 mm
BACKUP SLIDE

## Slide 23: TORSION FIT
The 2d map is fitted through a parabolic function:
Now we correct the effect of torsion using the parameter found for each bin:
instead of the Lindhard cut we will use
BACKUP SLIDE
Notes: This allowed us to apply a continuous torsion correction. So, instead of using a standard Lindhard cut centered at zero, we corrected the incoming angle using the fitted parameters found for each spatial bin.

## Slide 24: ANOMALOUS RUN 8650
Due to an issue, the run was taken at 150 GeV instead of 180 GeV.
Wider channeling peak
  More multiple scattering
Lower efficiency
  De-channeling more likely at lower energies
Larger critical Lindhard angle
BACKUP SLIDE

## Slide 25: ANGLE SELECTION
cut
For each square bin:
variation of
select particles
compute
select that maximizes (through gaussian fit)
BACKUP SLIDE
Notes: If not considering any torsion correction: we would just calculate the channeling efficiency through several iterations varying until the highest efficiency is found, representing the best alignment of incoming particles with the crystalline planes
If not considering any torsion correction: we would just calculate the channeling efficiency through several iterations varying 𝜃_0 until the highest efficiency is found, representing the best alignment of incoming particles with the crystalline planes

## Slide 26: ANGLE SELECTION
For each square bin:
variation of
select particles
compute
select that maximizes (through gaussian fit)
BACKUP SLIDE

## Slide 27: EFFICIENCY CURVE
Crystal efficiency as a function of the incoming angle, after application of the torsion correction. The value of the peak is the efficiency of the crystal when it is perfectly aligned to the beam.
BACKUP SLIDE
Notes: Applying this torsion correction significantly improves our analysis. When we plot the crystal efficiency as a function of the torsion-corrected incoming angle, the peak of this curve represents the efficiency of the crystal when it is perfectly aligned to the beam, which in this case reached 18.8%.